FMMS Paving requirements (RFP 20-024)

1. Clean existing track to remove dirt and debris.
2. Clear and laser grade a new lane to give the track a total of three lanes.
3. Install a stone base for new lane, compact to 95% standard proctor, and laser grade.
4. Install geo-textile fabric over structural cracks, if any of the existing track is reused.
5. Apply a tack coat at an application rate of 0.05 gal/sy to running track if any portion is reused.
6. Install a 1” Permaflex asphalt binder course to running track.
7. Install a 1.25” type II asphalt topping to running track and high jump pad.
8. Layout and stripe running track.
9. Build a 3’ asphalt long jump lane and sand pit beside track. Grade, Stone base and 1.5” asphalt binder course and 1.25”type II asphalt topping and compact.